**Dimensions**:            On the roll 1.2 X 12m or cut to size in spaghetti mats

**Thickness**:               14 mm +/- 1 mm

**Weight**:                    5,1 kg/m²

**Material**:                   100% PVC with enforced mesh backing.

**Application**:             Inside or outside entrance in a mat well or on top of an existing floor

……………………….with [edging](http://www.debomat.net/eng/top/products/edging/).

**Cleaning**:                 Vacuum clean regularly and shake out or hose down with water.

**Traffic:**  High - any level of foot or lightweight wheeled traffic.

**Colors**:                     Grey, Charcoal, Black, Navy Blue, Brown, Red.